### Key Recommendations for Addressing Failing Binders

- Timely Sampling and Testing:

  - Implement a 7-business-day turnaround for testing and reporting of field and terminal binder samples.

  - Collect and send the initial project binder sample to the Central Lab immediately after sampling.

  - Update the Engineering Policy Guide (EPG) to:

    - Reflect current sampling and testing practices.

    - Remove the requirement to wait for 10 samples before shipping.

  - Develop and implement protocols for truck blending sample approval.

  - Require MoDOT inspectors to witness or collect terminal samples.

- Recycled Engine Oil Bottoms (REOB) and Vacuum Tower Asphalt Extenders (VTAE):

  - Ban the use of REOB and VTAE to improve mixture quality and performance, aligning with neighboring states and FHWA recommendations.

- Poly Phosphoric Acid (PPA):

  - Maintain current practices for PPA use but require binder suppliers to disclose its usage to account for potential chemical interactions with amine-based anti-strip additives.