Bituminous Technical Team Meeting Agenda

May 6th, 2025 – (9:30 a.m. – 11:30 a.m.)

1617 MO Blvd. Jefferson City, MO  65109

Upstairs Conference Room 201

Topics

- BMD Specification Update

  - Sampling procedure updated to AASHTO R90

  - Added back aggregate comparison limits in Section 403.18.3.1 as it is referenced in other parts of the specification

  - Chart change for testing

  - Added gradation and deleterious to run on an “as needed” basis which wasn’t previously in the table but the current Section 403 requires to be run on a set frequency

  - Removed some redundant wording in Section 403.23.4 that is clarified later

  - The intelligent compaction adjustment removed to clarify that the adjustment only applies if the IC JSP is included in contract requirements

  - Wording on GNSS obstructions clarified

- BMD Round Robin Study for SP190 mixes

  - Working out details of a research project for round-robin BMD testing of base mixes to compare lab to lab variability of all MoDOT labs.

  - Study to include 3 different SP190 mixes from 3 projects

  - Looking at making a set of pucks without re-heating at each project and then sending loose mix to all 7 districts and central lab to be re-heated the same.

- BMD Pay factor sheet update

- Draft sheet available, project offices will need to request a copy from the field office when they need it

- Limited distribution to hopefully iron out all the bugs before a more widespread release

- HiMod Asphalt Spec

  - 90% recovery (MSCR recovery) with a 76E-28

  - Rotational viscosity bumped up to 3.5 max (was 3.0) – contractors can go lower if they suspect higher viscosity binder will cause constructability issues

  - Utah has been using Hi-Mod the most and are at 3.0 maximum and increased hose sizes and don’t have issues

  - Virginia has allowed a 5.0 max on viscosity but we have no information on if their performance went well or not

  - Minimum binder content table established

  - Will monitor, esp. in SE district

  - Maximum 15% binder replacement

  - Not allowing river gravels or natural sands

- Updates to 1015 for eliminating REOB and VTA

  - Section 1015.3.1 is for PPA to be noted on the bill of lading if used in the binder so contractors know

  - Section 1015.10.1 Refined engine oil bottoms and vacuum tower asphalt extenders are no longer allowed in PG binders.

  - MAPA researching practices from other states on these issues

- BMD for low volume roads

  - How would BMD work for low volume routes?

  - Just mix design stage and once during production maybe?

  - BMD production checks would probably require a Gmm test to make sure sample air voids are correct.  Using the JMF Gmm might not be sufficiently accurate

  - Void requirement similar to Superpave in lieu of BMD testing during production, but would this prevent early thermal cracking?

  - Density testing of low volume mixes?

  - Possibly modify this, maybe combine with volumetric testing for low volume mixes

  - Add Gmm testing during production to increase accuracy of production density testing - Would still add an hour or two to testing

  - Modification to testing protocols would increase bid prices

  - MAPA to discuss internally for their perspective

  - Alabama Counties have worked with NCAT to develop a “lightweight” BMD specification

  - Basically CT index and high temperature IDT (comparable to RT index)

  - In summary, MoDOT looking to implement BMD in some form for low volume routes instead of more research on effects of RAP/RAS

- Addressing flushing/bleeding Issues and surface defects

  - Issue could be caused by gradation issues

  - Comments from Mark Blow on the topic, various sieves mentioned (#200, #4, #8 etc.) but primary focus was how clean the mixes were

  - Research project in SE district on I-55 J9I3838

  - Project limits below with intent to have 4 test sections to compare against the SP095B

  - Possible test sections, following are ideas that may be used.  Final test sections to be determined

    - SMA with Hi-Mod

    - SMA with BMD

    - SP095B with Hi-Mod

    - ??

  - One idea is to use an SMA mix with BMD specs such that the oil content could be backed down below 6.0%

  - Possibly use hi-mod asphalt though the high polymer binder hasn’t been used in SMA to MoDOT’s knowledge

  - Utah’s Hi-Mod specification is for dense-graded asphalt but also has a drain-down requirement

  - Side discussion on using GTR w/ or w/o fibers in SMA?

  - For now, fibers required as a “cheap insurance” per results from an SMA mix using dry-process GTR but still had fibers

- Flint Chat vs High Chert Content

  - There has been poor field performance of mixes where flint chat is used in lieu of porphyry and the limestone fraction had a high chert content

  - Early raveling and stripping

  - It was brought up that this could be due to not enough binder in the mix

    - A spec. would need to be developed to ensure adequate binder is in the mix.

  - Proposing limiting the total chert content in the limestone to 5% of the mix when flint chat is used in lieu of porphyry (e.g. SMA or LP mixes)

  - Stop-gap measure to mitigate concerns with using chat pending further research/discussion

  - Concerns/Questions:

  - What about counting chert as non-carbonate in lieu of chat?

  - Chert content fluctuations making mix harder to control?

  - Chert quality not as uniform as chat, e.g. hard chert vs. soft chert in the limestone

  - Mixes may have needed more asphalt due to the angularity of the chert & difficulty in compaction

- Volumetric Comparison Limits

  - Comparison limits match what they were when Superpave began

  - At the time (late 90’s) AASHTO multi-laboratory acceptable range of two results were very high and MoDOT used lower values

  - Concern of too many n=5 instances for QC/QA

  - Request for MoDOT to compare specification requirements vs. AASHTO standards for limits of favorable comparison

- TSR Replacement and Stripping Test Research Study

  - Presentation by Punya Rath presenting the results of the study

  - Compared TSR & Hamburg results to see which better predicted stripping susceptibility

  - Hamburg analysis for stripping potential depends on the slope ratio first, if =< 2.0 mix is ok, if >=2.0 the stripping inflection point is calculated

  - If stripping inflection point (SIP) <= 15,000 passes and slope ratio (SR) >2.0 mix is susceptible to stripping

  - Concerns about moving forward with Hamburg in lieu of TSR:

  - would effectively require all contractors get a Hamburg testing machine

  - significant impact to industry

  - Hamburg test more cumbersome to run vs. TSR test

  - Hamburg test equipment more of a maintenance burden and requires more capital investment from contractors

  - However, Hamburg seems to be a more reliable indicator of stripping potential compared to the TSR test

  - Alternative of running RT index on tests conditioned according to TSR requirements for wet set pucks?

    - Not done yet, could be researched

  - What about running only one pair of pucks for stripping test so two separate mixes could be evaluated simultaneously?

    - If wheels operate independently, it is a feasible approach but would have only 1 result per sample, wouldn’t get the replicate result from other wheel path for the sample