SUBMITTED & APPROVED – EFFECTIVE OCT 2025

403.13.1 Uneven Lanes. For roadways constructed under traffic, uneven pavement lanes shall not be left in place for more than seven days, unless approved by the engineer.

403.13.1 Uneven Lanes. For roadways constructed under traffic, uneven pavement lanes shall not be left in place for more than seven days, unless approved by the engineer.

NOT SUBMITTED – EFFECTIVE JAN 2026

403.13 Spreading and Finishing. The base course, primed or tacked surface, or preceding course or layer shall be cleaned of all dirt, packed soil or any other foreign material prior to spreading the asphaltic mixture. If lumps are present or a crust of mixture has formed, the entire load will be rejected. The thickness and width of each course shall conform to the typical section in the contract. The contractor may elect to construct each course in multiple layers, with minimum compacted lift thicknesses equal to 4 times the nominal maximum aggregate size, unless otherwise shown on the plans.  The minimum compacted lift thickness for the top lift surface course shall be 1.0 inches for SP048, 1.5 inches for SP095, and 2.0 inches for SP125.   The minimum compacted lift thickness for base mixtures shall be 3.0 inches for SP190 and 4.0 inches for SP250 mixtures.