## Slide 1
MoDOT Field Office Update

## Slide 2: Highly Modified Asphalt (HiMod)
Highly polymer modified binder
Results in a very crack and rut resistance mixture
High Performance - Comparable to SMA performance
  But a dense graded mix
  Instead of relying on high quality aggregates HiMod relies on the high amount of polymer in the binder

## Slide 3: Key HiMod Mixture Characteristics
50 gyration mixture
0.5 to 1.5 percent air voids
90% MSCR recovery
Jnr max of 0.1
Minimum 6% AC
Hamburg– max. 7mm of rutting @ 20,000 passes w/ 4% air voids

## Slide 4: Recent HiMod Changes
Increased allowable viscosity from 3.5 to 5.0 max
Reduced gyrations from 65 to 50
Allowed air voids to be reduce to 0.5
Required the binder to be modified by Polymer

## Slide 5: HiMod Thick Lift Paving
Being a very rich mix HiMod is easy to compact
Allows for paving thicker lifts
Improved performance from having less interfaces
  Not relying on tack for bonding
Quicker operation

## Slide 6: HiMod Thick Lift Paving
Smoothness becomes a challenge
Top surface only allowed to be diamond grinded
Base course allowed to be micro-milled
  Cold milling not allowed due to generated excessive fines
Top lift also much be a level B or low porphory mixture
HiMod mixtures only 12.5 or 9.5 mm

## Slide 7: HiMod Full Depth Thickness
Currently MoDOT allows 25% reduction from regular superpave with improved subgrade
NCAT currently recommends about 40% reduction
Research is needed to know exactly
Recalibration of AASHTO ME design needed

## Slide 8: 2026 HiMod Pilot Projects
J9I3838 I-55 – small test section
  January Letting
KU0198 I-49 2 inch overlay
  April Letting
  Over 18 lane miles

## Slide 9: BMD Update
No major specifications changes made in 2025
Spec. needs some tweaking before full implementation
  Too much testing
  RT index failures on 64V-22 binders
  Aging Maters

## Slide 10: Unacceptable BMD Mixture that Passes Current Specification
JMF | CT Specimens Made Early | CT Specimens Made Later
JMF CTIndex= 127.2 JMF CTIndexLong-Term = 20.8 | 175.7 | 52.3
 | 136.6 | 46.9
 | RT Specimens Made Early | RT Specimens Made Later
 | 48.7 | 76.3
 | 50.7 | 74.8

## Slide 11: What is Asphalt Aging?
Loss of effective binder in the mixture
  Absorption of asphalt into rock reducing the effective binder content resulting in a stiffer more brittle mix.
  Oxidation of the asphalt binder
    A chemical process in which binder reacts with oxygen resulting in the degradation of the asphalt binder
    Results in a stiffer more brittle mix

## Slide 12: Factors Effecting Aging
Absorption of rock
Amount of AC in mixture
Amount of binder oxidation - Temperature and Oxygen
Air voids of mixture
Chemistry of asphalt binder

## Slide 13: Easiest Way to Reduce Aging
Ensure there is enough AC in the mixture
Achieve high density on the roadway to reduce air voids
  Reduces oxidation of the asphalt binder

## Slide 14: MoDOT’s Long Term Aging
20 hours at 115°C
Represents about 7 to 8 years of aging in the field
Goal of 10 year life for overlays
Still need some performance at year 7 and 8

## Slide 15: MoDOT’s 2025 Long Term Aged CT
Average = 39.2 with a std. deviation of 20
Range of 16.2 to 80
Long term performance is main goal of BMD so our specification needs to capture this
For reference: BMD Spec. requires unaged minimum CT index to be minimum of 50 for non-sma with above 100 for bonus

## Slide 16: 2025 JMF Results
Avg CT Index | Avg Long Term Aged < 30 | % Difference
77.9 | 35.5 | 54
117.2 | 76.5 | 35
95.8 | 60.2 | 37
98.9 | 30.6 | 69
83 | 21.2 | 74
123.2 | 16.2 | 87
140.2 | 56.5 | 60
82.3 | 41.9 | 49
127.2 | 20.8 | 84
228.4 | 31.9 | 86
129.3 | 56.4 | 56
63 | 32 | 49
103.1 | 75.3 | 27
140.3 | 32.6 | 77
61.7 | 31.4 | 49
132 | 47 | 64
Notes: Long Term Age – 20 hours at 115 C – to about year 7 or 8.

## Slide 17: Long Term Aging Research needed.
What’s the min. CT value needed at year 7 or 8?
  Field test sections take 10 years to validate
  Can lab testing give us a starting point?
  Design mixture with low CT values to see what number we start to see cracking?

## Slide 18: Failing RT of 64V Binders
PG Grade High Temperature* | Minimum RTIndex
58-28H / 64-22 | 50
64-22H / 70-22 | 65
64-22V / 76-22 | 80

## Slide 19
Chart: 
| All Mixes | PG64-22 | PG70-22 | PG76-22
 | 8 | 17.3 | 8.1 | -4.1
Notes: Rt min. 64 – 50 64H – 65 64V - 80

## Slide 20: 2025 JMF Results Failing RT of 64V Binders
Not seeing an increase in RT from 64H to 64V binders
Is it a binder issue or a testing issue?
Are we not allowing the mix to age enough?
Are we getting the field performance we need?
More research is needed..

## Slide 21: Failing RT in the Field
Currently requires verification of Hamburg results with reheated mix
Typically, have seen no rutting
Should we just plan to run the Hamburg?
  Could replace TSR with the SIP to reduce testing
More research needed for both

## Slide 22: Plan for Reducing Testing
Look at reducing testing frequencies
  Low frequencies increases risk to contractor
Possibly combine some testing?
  Stripping with the Hamburg
  Consistent CT to trigger rutting check

## Slide 23: BMD Spec. Moving Forward
Continue with additional pilot projects in 2026
Complete Research in 2026-2027
Spec. revisions in 2027?

## Slide 24: Intelligent Compaction of Asphalt
North West District Pilot Projects
  Pays Contractor 3 % for the IC Data – Requires complete data
    Paving will cease if optimum passes not achieved for two consecutive paving days or if daily production has less than 70% coverage.
    Integral Shoulders will be checked to see if optimum rolling passes were used.
      If so, no further action
      If not, then additional testing will be conducted with the contractor correcting or remove and replaced based on density results.

## Slide 25: Intelligent Compaction of Subgrade and Base Rock
2 Pilot projects scheduled for 2026
Can we compare ICMV to a CBR value
  ICMV much deeper depth of influence
QA could be LWDs
Could replace proof rolling

## Slide 26
Mounting DPS unit to rollers has been successful
  Both break down and finish rollers
  Just can’t have ponding water
A lot of interest from other states
MoDOT member of pooled fund and plan to continue to monitor
Dielectric Penetrating System (DPS)

## Slide 27: Questions?