## Slide 1: Missouri Asphalt Pavement Association (MAPA) Endowed Professorship Update
By: Magdy Abdelrahman, Ph.D.
Missouri University of Science and Technology
2025 Annual MAPA Conference
January 7th, 2027

## Slide 2: Missouri S&T Updates, Research
Testing alternative binders for HFST.
  Standard PG Binders, Example, PG 82-22
  Emulsion, Modified and Regular,
  Lab Developed Modified Binders, PG88-16(PM)
Currently, Develop Emulsion-Based bio binders & Use of recycled oil, environmental concerns in the planning phase.
Crumb rubber optimization, adding rubber to the asphalt line to produce wet-process binder
Friction Testing, AASHTO - AASHTO Innovation Initiative - Dynamic Friction Testing with Three Wheel Polishing Device (transportation.org)

## Slide 3: Friction Testing Equipment
BP System
DFT &
C-Meter

## Slide 4: Objectives
Missouri University of Science and Technology
- Develop and optimize different asphalt binders as alternatives for HFST.
Binder Type | Details
Unmodified Binder * | PG88-16 & PG94-10
Polymer Modified Binder (SBS) * | PG88-16(PM) & PG82-22(PM) “Kraton polymer modifier”
Emulsion * | CRS-2P & CRS-2PSC
CRM Binders ** | 6 CRMBs
* MoDOT Report (2024). ** New Developed Binders. | 
Table1. List of Conducted Asphalt Binders for HFST

## Slide 5: CRM Binders
Missouri University of Science and Technology
Main Goal:
Crumb Rubber Modifier (CRM) binders in HFST .
Develop an understanding of how binder rheology and interaction conditions
influence HFST microtexture durability and polishing resistance.
Why CRM?
  CRM binders can provide the elasticity, stiffness, and durability required for HFST.
  Crumb rubber offers a proven performance history in asphalt pavements but has never been fully explored for HFST.
  CRM supports sustainability by recycling waste tire rubber and may reduce reliance
on expensive epoxy binders.

## Slide 6: Experimental Testing Plan
Three Wheel Polishing Device (TWPD)
Missouri University of Science and Technology
Testing Plan
Asphalt Binder Testing
HFST Performance Testing
Rheological Testing
Bonding Testing (Pull-off)
Frequency Sweep
Temperature Sweep
British Pendulum Test (BPT)
Dynamic Friction Test (DFT)
Circular Track
Meter (CTM)
Polished Stone
Value (PSV)

## Slide 7: Materials (cont.)
Missouri University of Science and Technology
Preparation of CRM Binders
Crumb rubber types: wet ambient type (30A) and cryogenic type (40C).
Interaction temperatures: 170 °C and 200 °C.
Crumb rubber (CR) content %: 10% and 15%.
Interaction shear mix speed and duration: 3000 rpm & 4 hours.
Table 2. Identification and Specifications of the Investigated Asphalt Binders
Binder IDs | CR Type | CR, % | Temp, °C
Base Binder | ــــــــ | ــــــــ | ــــــــ
CR 30A-15-170 | 30A | 15 | 170
CR 30A-15-200 | 30A | 15 | 200
CR 40C-10-170 | 40C | 10 | 170
CR 40C-10-200 | 40C | 10 | 200
CR 40C-15-170 | 40C | 15 | 170
CR 40C-15-200 | 40C | 15 | 200

## Slide 8: Bitumen Bond Strength (BBS)
Conditioning
Purpose
Evaluate the adhesive strength between asphalt-based binders and aggregate and substrates.
Assess resistance to debonding under environmental and mechanical stresses.
Importance
Ensures binder bonding efficiency and validates the quality of developed binders.
BBS device

## Slide 9: Results and Discussion (cont.)
Missouri University of Science and Technology
Comparison with Traditional Epoxy Resin
Table 3. Friction and Texture Performance between Epoxy-Based and Investigated Asphalt-Based Using CB Aggregate
Source/Reference | Binder Type | 140k Polishing Cycles |  | Post BPN
 |  | COF50 | MPD | 
Roshan and Abdelrahman, (2025) | Epoxy Resin | 0.62 | 1.85 | 61
 | PG88-16(PM) | 0.59 | 1.10 | 58
 | PG82-22(PM) | 0.64 | 1.40 | 58
 | M2 | 0.65 | 1.95 | NA
New Developed Binders (CRM) | Base Binder | 0.60 | 1.14 | 65
 | CR 40C-15-170 | 0.62 | 1.21 | 71
 | CR 40C-15-200 | 0.66 | 1.11 | 72

## Slide 10: CE3116 Construction Materials, Properties and Testing including Labs Spring &Fall 2025
Origins, production, properties, types, and uses of construction materials accompanied by selected laboratory tests
Instruction Mode
Classroom Based
Over of 100 students/year
Adopts Based on the NCAT Textbook

## Slide 11: CE5112 Bituminous Materials and Mixtures, Online, including Labs Fall 2025
Properties, types, and grades of bituminous materials are presented. Emphasis is placed on usage, distress, and asphalt concrete mix properties, behavior, design, manufacture, and construction
Instruction Mode
Classroom Based
Record enrollment, 37 students
Based on the NCAT Textbook, Thanks to MAPA

## Slide 12: CE6123 Pavement Management, Evaluation and Rehabilitation
Spring 2026
Advanced knowledge of pavement performance; pavement evaluation; implementation of pavement management at network and project level; maintenance and rehabilitation strategies; life-cycle-cost analysis
Instruction Mode
Classroom Based
On-line Synchronous
Based on the PAVER system and software (US Army Corps of Engineers)

## Slide 13: Presentations, the 105th TRB Annual Meeting, 2026
Roshan, A., and Abdelrahman, M. (2026). “A Novel Combined Degradation Index for Long-Term Performance Comparison of Epoxy and Asphalt-based High-Friction Surface Treatments (HFST).” The 105th Annual Meeting of the Transportation Research Board (TRB). Paper No. TRBAM-26- 03498.
Hemida, A., El-Ashwah, A., and Abdelrahman, M. (2026). “Innovative Use
of Used Motor Oil as a Rejuvenator in Sustainable Asphalt Binders
Containing Guayule Resin and Crumb Rubber.” The 105th Annual Meeting of the Transportation Research Board (TRB), Paper No. TRBAM-26-05358.

## Slide 14: Thanks to MAPA for Supporting my Work
Questions?
Contacts:
Magdy Abdelrahman, Ph.D.
Associate Chair for Graduate Studies and Research and
Missouri Asphalt Pavement Association (MAPA) Endowed Professor
Civil, Architectural and Environmental Engineering
Missouri University of Science and Technology
134 Butler-Carlton Hall 1401 N Pine St.
Rolla, MO 65409-0030
Ph. (573)341-6124
m.abdelrahman@mst.edu