Bituminous Technical Team Meeting Notes

July 28, 2026 – (9:30 a.m. – 11:30 a.m.)

1617 MO Blvd. Jefferson City, MO  65109

Upstairs Conference Room 201

Topics

- Review October 2026 Specification Updates (See attached presentation slides)

  - Sec 1015 – PPA

    - Limits the amount of polyphosphoric acid (PPA) to 0.25% by weight of binder

    - Comment from industry that other agencies, when requiring MSCR, have % recovery or % elastic recovery – will discuss if MoDOT should consider

  - Sec 406 – PMTP

    - Previous JSP rolled into Specification as Sec 406

    - Small quantity for PMTP may need further explanation in the specification

      - PMTP might not work well in staged construction, small quantity, etc.

  - Sec 403 – BMD

    - BMD JSP was incorporated into Sec 403

    - MoDOT allowed the transfer of previously approved SP190/SP250 mixes with 4% air voids to contracts requiring 3% air voids

      - An approved SP190/SP250 mix with either 60 gyrations or 80 or 100 gyrations can be transferred to contracts with the new spec until the mix expires

    - Discussion that the BMD gyrations should be “minimum 60” instead of equal to 60 as presented

      - * After the meeting concluded, it was verified that this was included in the final Sec 403 language

    - RT index vs. Hamburg results for mix design approval

      - Allowing the HWT to govern if the RT doesn’t meet minimum

    - Discussed changing the testing frequencies:

      - Can the frequency of QC gradation be reduced to 1/lot  - will consider

      - Consider adding PMTP guidance for small quantities in Sec 403

    - Change to adjustments spreadsheet

      - Allow variable target for minimum RT index

- RT/HWT Correlation

  - Intent is to run the HWT and compare against the RT index

  - If RT index = 58, RT  > 58 ok, if RT = 52 then you re-run the HWT

- Review January 2027 Proposed Specification Update

  - Sec 410 – Single Lift Overlay

    - Clarified when single-lift overlay requirements apply based on the depth of cold milling

      - If < 1” cold-milling the spec applies the smoothness requirements of a single-lift overlay (“scratch mill & overlay”)

      - Concern was mentioned that % improvement with a “scratch mill & overlay” may be problematic if the road was relatively smooth before the project.  Hard to get a 30% improvement if the road is already smooth (IRI < 80)

    - Re-worded specification for clarity otherwise

- Other Topics

  - Were there any Hi-Mod binder specification changes?

    - Hi-Mod not in specification yet, no updates to the Hi-Mod JSP at this time